## Slide 1
Measuring Metal Release Rate from an Arsenopyrite Sample
Chemistry of Metal
Sulfide Minerals

## Slide 2: Sulfide Minerals
Pyrite (FeS2)
“Fool’s Gold”
Pyrite and Marcasite (FeS2)
Arsenopyrite (FeAsS)
Covellite (CuS)
Chalcopyrite (CuFeS2)
Galena (PbS)
Wurtzite, Sphalerite (ZnS)
Found near metal ore and coal deposits
Exposure to air and water causes oxidation and subsequent dissolution
Sulfuric acid produced
Metals leached from surrounding minerals
} Acid Mine Drainage

## Slide 3
Wisconsin Territory, 1836
Notes: The names of places such as Galena and Mineral point reflects those part of the history of

## Slide 4
Lead Mines in Wisconsin-Illinois, 1829

## Slide 5
Wisconsin State Flag
A miner and a pile of lead cannonballs
feature prominently in the Wisconsin flag

## Slide 6
Madison
Fond du Lac
Appleton
Oshkosh
Milwaukee
Green Bay
Wells with [As] > 5 ppm in Wisconsin

## Slide 9
pH=2.05
Well was constructed in 1977. In 1990, homeowners reported that water was irritating their skin, had a metallic taste, and was deteriorating plumbing fixtures. The Wisconsin DNR found that…
[As] > 4300 ppb
[Cr]=84 ppb
[Cd]=220 ppb
[Ni]=11,000 ppb
[Pb]=400 ppb
Fox valley arsenic problem: Example

## Slide 10: Arsenic Poisoning in Bangladesh
Estimated that ~65 Million people are exposed to high As concentrations from naturally-occuring arsenopyrite

## Slide 11
Arsenic Poisoning in Bangladesh

## Slide 12
http://www.washingtonpost.com/wp-dyn/content/article/2007/02/01/AR2007020101874.html
http://pubs.acs.org/cen/news/85/i07/8507prize.html

## Slide 13
AMD (Acid Mine Drainage)
Sulfide minerals are found at coal and metal deposits. Mining exposes the sulfides to air and water, which results in their oxidative dissolution. This leads to the generation of sulfuric acid and release of heavy metals into water supplies, the process is known as acid mine drainage.
Picture of Iron Mountain Mine, in northern California.
It was mined for iron, silver, gold, copper, and zinc beginning in the late 1800’s till 1962. It was identified by EPA as the largest discharger of toxic metals in US.

## Slide 14
Green water, due to Cu2+ , Ni2+
Inside Iron Mountain
pH < 1
High metal concentrations
  Fe > 21,000 mg/L
  Zn > 2000 mg/L
  Cd > 16 mg/L
  Cu > 200 mg/L
  As > 47 mg/L
Temperature ~ 50°C

## Slide 15
55 million tons of ore from a sulfide mineral deposit that is approximately 4,900 feet long, 2,200 feet deep and 100 feet wide. The total surface area disturbed during mine development would be about 550 acres.
Proposed Crandon Mine
in Northern Wisconsin

## Slide 16: Sulfide Minerals
Pyrite (FeS2)
“Fool’s Gold”
Pyrite and Marcasite (FeS2)
Arsenopyrite (FeAsS)
Covellite (CuS)
Chalcopyrite (CuFeS2)
Galena (PbS)
Wurtzite, Sphalerite (ZnFeS)
Found near metal ore and coal deposits
Exposure to air and water causes oxidation and subsequent dissolution
Sulfuric acid produced
Metals leached from surrounding minerals
} Acid Mine Drainage

## Slide 17
Pyrite (FeS2) - most abundant sulfide- model system
What is known about metal sulfide dissolution?
Pyrite: Similar crystal structure to NaCl (Alternating positive Fe2+ with S2-2 “dumbbells”)
How does pyrite react?
Used as a model system for understanding metal sulfide chemistry.

## Slide 18
FeS2+ 14Fe3++ 8H2O =>15Fe2++ 2SO42- +16H+
23 molecules on left-hand side of the equation !
14 Ferric ions required just to oxidize one FeS2
Implication:
Reaction must proceed through a series of steps.
What are they, and where do they occur (surface or in solution?)
The balanced equation:
What is known about metal sulfide dissolution?
Fe2+ is stable in solution, but S-1 (and As-1) are not
Implication: All metal sulfide reactions involve oxidation of the sulfur and/or arsenic species
We can not realistically expect a reaction to involve simultaneous collision of 23 reactants!

## Slide 19
There are two general pathways for pyrite dissolution at pH<3:
FeS2 + 7/2 O2+ H2O => Fe2+ + 2SO42- + 2H+ (1)
FeS2+ 14Fe3++ 8H2O =>15Fe2++ 2SO42- +16H+ (2)
While O2 and Fe3+ are two competing oxidants, isotope studies show that oxygen in sulfate comes mainly from water. This shows that Fe3+ as the direct oxidant, and O2 probably regenerates Fe3+ through:
[Taylor, B.E.; Wheeler, M.C.; Nordstrom, D.K. Geochim. Cosmochim. Acta 48, p2669-2678.]
Fe2++1/4O2+H+ => Fe3++1/2H2O
What is the oxidizer?

## Slide 20
yFe2+
FeS2
FeAsS
O2
xFe3+
(x+1)Fe2+
FeS2
FeAsS
O2
xFe3+
Fe2+
Fe3+
Surface
reaction
Solution
reaction
Catalytic cycling of ferric ion
Oxygen affects reaction by regenerating Fe3+ in solution.
Oxygen does not directly react at the surface!

## Slide 21
One possibility (out of many):
FeS2 + 6Fe3+ + 3H2O ------7Fe2+ + 6H+ +S2O32- Thiosulfate as intermediate on surface
S2O32- + 8Fe3+ + 5H2O ------ 2SO42- + 8Fe2+ + 10H+ Oxidation of thiosulfate to sulfate
in water
S-1 (or S2-2 ) in mineral (Sulfur = -1 oxidation state)
S8 (elemental sulfur) (Sulfur= 0 oxidation state)
S2O32- Thiosulfate (Sulfur = +2 oxidation state)
SO32- Sulfite (Sulfur = +4 oxidation state)
SO42- Sulfate (Sulfur = +6 oxidation state) --- The final product
Sulfur oxidation states:
How does the sulfur get oxidized?
Note that elemental sulfur (S8) is not soluble in water

## Slide 22: “Local” Dissolution Model
Moses and Luther proposed that in low pH solution, the electron
transfer occurs between the surface and the hydrated ferric ion, this
cycle repeats until the oxidized sulfur compounds leaves the surface.
Fe
S
S
e-
Fe
S
S
Fe
e-
Fe
S
S
O
O
Fe
S
S
O
O
Fe
S
S
O
O
[Moses, C.O.; Nordstrom, D.K.; Herman, J.S.; Mills, A.L. Geochim. Cosmochim. Acta 51, p1561]
[Luther, G.W. Geochim. Cosmochim. Acta 51, p3193]
Fe
Fe

## Slide 23
FeS2
FeAsS
2Fe3+
FeSSO
FeSSO2
7Fe2++
2SO42-
2Fe2+
2Fe3+
2Fe2+
FeSS
2Fe2+
2Fe3+
8Fe3+
FeSSO3
}
S2O3
(Thiosulfate)
FeS2 + 14Fe3+ + 8H2O ------15Fe2+ + 16H+ +2SO42- Sulfate as end product
Break down into two steps:
FeS2 + 6Fe3+ + 3H2O ------7Fe2+ + 6H+ +S2O32- Thiosulfate produced at surface
S2O32- +8Fe3+ + 5H2O ------8Fe2+ + 10H+ +2SO42- Thiosulfate to sulfate oxidation
7Fe2+
S2O3 2-

## Slide 24
FeS2
FeAsS
2S0
FeSS
3Fe2+
2Fe3+
FeS2 + 2Fe3+ 3Fe2+ + 2S Elemental sulfur (S8) as end product
S8
Fe3+
X
No Reaction!
Formation of
elemental sulfur is
important because
elemental sulfur
can block ability of
Fe 3+ to get to the
Surface !
Another issue: What is the role of elemental sulfur?
Elemental sulfur does not appear to be a major intermediate during pyrite oxidation. However, it does appear to be a major product from other sulfides, such as arsenopyrite (FeAsS) and galena (PbS) .

## Slide 25
Influence of pH :
FeS2+ 14Fe3++ 8H2O =>15Fe2++ 2SO42- +16H+ (2)
According to “Le Chatelier’s Principle”, increasing [H+] (lowering the pH) should push the equilibrium toward the left.
However, the maximum concentration of Fe 3+ in solution is controlled by its solubility product
Fe3+ + 3 OH-  Fe(OH)3
If Fe(OH)3 is present (high pH), then as the pH goes down, the amount of Fe 3+ that can stay in solution increases. So, the rate of the reaction increases.
But what effect does H+ have at lower concentrations, where
Fe(OH)3 precipitate does not form?

## Slide 26
yFe2+
FeS2
FeAsS
O2
xFe3+
(x+1)Fe2+
FeS2
FeAsS
O2
xFe3+
Fe2+
Fe3+
Surface
reaction
Solution
reaction
Removal of Fe3+ by precipitation of Fe3+ at high pH
OH-
Fe(OH)3 (solid)

## Slide 27
A Few Potential Variables:
Ferric ion concentration:
Fe3+ needed to induce reaction, Fe2+ is a product
Total [Fe] increases during reaction
Presence/Absence of oxygen:
Oxygen converts Fe2+ to Fe3+
Does oxygen have any “direct” Role in the reaction?
Temperature:
Is reaction faster at elevated temp?
“Iron Mountain” produces H2SO4 at 40-50oC.
pH:
Does pH affect reaction only through solubility of Fe(OH)3?
Ferrous ion concentration:
Does concentration of ferrous ion affect reaction rate?

## Slide 28: Goals of the Design Project
Learn quantitative analysis in the context of a real-life environmental problem.
Learn how to apply the scientific method as you develop hypotheses, design your experiments, and develop your own interpretation.
Understand some of the complexities and uncertainties associated with scientific measurements, especially when working with complex systems and the natural environment.
Learn how to communicate your scientific results, orally and in writing.
Are for you to:

## Slide 29
What controls the rate?
Ferric ion concentration:
Overall stoichiometry involves large number of Fe3+ ions.
What is the order “n” of the reaction? (Rate ~[Fe3+]n)
Ferrous ion concentration:
Electrochemical potential of an electrode is controlled by ratio of concentrations (Fe3+ / Fe2+). Even though the reaction is strongly “downhill”, it is still possible for a product to strongly affect the rate.

## Slide 30
What controls the rate?
Presence/Absence of oxygen:
Oxygen converts Fe2+ to Fe3+
Does oxygen have any “direct” Role in the reaction?
Temperature:
Is reaction faster at elevated temp?
“Iron Mountain” produces H2SO4 at 40-50oC.
pH:
Does pH affect reaction only through solubility of Fe(OH)3, Le Chatelier’s principle says that since H+ is a product, lowering the pH should shift the equilibrium toward the reactants. However, the system is far from equilibrium…

## Slide 31
How can you learn about the mechanism of a reaction?
1) Measure the rate of reaction !
Determine how the rate of reaction depends on certain key variables such as [H+], [Fe 3+ ],
Presence/absence of oxygen, etc.
Kinetic measurements typically give good information about the slowest step(s) in a chemical reaction. Those are usually the steps that of the most interest.

## Slide 32
Kinetics of chemical reactions:
A + B C
Rate constant
time
Slope of this line is the rate =
The simplest example:
Rate when [A] is lower
Rate when [A] is higher

## Slide 33
A + B C
Rate constant
time
Slope of this line is the rate =
The simplest example:

## Slide 34
Kinetics of chemical reactions:
2A + B C
For this mechanism, the slope of this line is the rate should be proportional to [A]2
More complicated:
time
This reaction is “second-order” in [A] and “first-order” in [B]
Can determine the “order” of a reaction, and how many atoms
Are involved in the rate-determining step, but measuring how the rate changes with the concentration of a reactant

## Slide 35
Measure the distribution of products !
FeAsS - Fe 2+ + S8(surface)  S2O3  SO4
S2O3
S8
SO4
Rate 1
Rate 2
Rate 3
By measuring the concentration of each intermediate as a function of time, we can develop a kinetic model that will tell us about the mechanism of the reaction

## Slide 36
Arsenopyrite (FeAsS)